| DESCRIPTION | A new era for interlinings. ‘GMP’ is a high-performance adhesive system from Lainiere France designed to deliver a super soft handle that easier to fuse with greater tolerance to fusing conditions. Providing less strike back and fantastic bond strength. |
| --- | --- |
| COLOURS | Black & White |
| WEIGHT WIDTH | 34 GSM 150cm |
| ROLL LENGTH | 100m per roll. |
| COMPOSITION COATING FUSING CONDITIONS CARE INSTRUCTIONS | 100% Polyester/ Polyamide GMP coated Dial Temp: 130 – 140 degrees Celsius Glueline Temp: 116 - 121 degrees Celsius Pressure: 20 – 30N/cm 2-3 Bar Time: 10-13 seconds Washable up to 40 degrees Celsius Drycleanable |

Fuse Knit 2416 ‘GMP’

The information contained in this performance specification sheet is subject to change without notice and remains the property of Charles Parsons and Co. It shall not be reproduced in whole or part, nor provided to any third parties without the written authorisation of Charles Parsons and Co. Charles Parsons and Co makes no warranty of any kind with regard to this technical specification, including but not limited to, the implied warranties of merchantability and fitness for a particular purpose. Charles Parsons and Co shall not be liable for incidental or consequential damages in connection with the supply, performance or use of this fabric. The previous conditions are only a guide. A preliminary trial is recommended before using the product in production